In piping, fit-up refers to the actions taken to assemble and align pipe components before welding or final assembly so that the joint:

·  Is in the correct orientation
·  Meets dimensional tolerances
·  Can be welded without defects
·  Will perform reliably in service

- Pipe & Fittings Fit-up:

- Visual Inspection
Inspect pipe visually and check condition.

- Position per Drawing

·  Position pipes per isometric drawing.

- End Prep (Bevel & Root)

·  Prepare ends with correct bevel angle (37.5 - bevel protector) & root face(1.6mm - vernier caliper).

- Root Gap & Alignment

·  The root gap (1.5-3mm - Taper gauge) and hi-lo( < 1.5mm - high-low gauge) should be correct

- Clean Weld Area

·  Clean weld area by removing paint/coating (20mm from the weld).

- Level & Centerline

·  Align & level pipes (Spirit Level).

7) Clamp & Tack

·  Tack weld the pipes in place by qualified welder.

8) Record & Approve

·  Record & approve fit-up before full welding.

- Flanges Fit-up:

- Inspect flange faces

· No damage and correct flange and face is used.

- Bolt hole orientation:

·  Bolt hole orientation should be correct the max bolt hole offset allowed is ±2.4mm

- Flange face tilt

·  The face must be parallel and tilt allowed is 0.025 mm per 25mm and max ≤  0.672 mm.

- flange face Seperation

- ·  The face must be aligned and max face separation allowed is ±1.6 mm.

- Gasket Inspection

·  Confirm gasket correct and fit properly before installation.

- Gaskets Fit-up:

- Verify Correct Type, Size & Rating:

·  Confirm that the gasket matches the flange class, temperature/pressure rating.

- Check Gasket Condition

·  Gasket must be clean, undamaged, without cracks, folds, tears or deformation.

- Clean Flange Contact Surfaces

·  Flange faces where the gasket sits must be clean, dry, and free of any contaminants (paint, rust, oil, debris)before installation.

- Inspect Bolt & Washer Compatibility

·  Bolt size, grade, thread condition and Washers appropriate for gasket type.

- Torque/Tension Monitoring:

·  Correct tightening sequence,Properly calibrated torque tools

- Bolts & Nuts Fit-up:

1) Verify Correct Bolting Materials

·  Check bolts, nuts, and washers against IFC drawing and specs (size, length, grade, class)and material grade markings match the material specification (e.g., ASTM A193, A194 per project requirement).

- Visual Inspection Before Installation:

·  Check condition of bolts, nuts & washers, No thread damage, or cracks

- Gasket & Flange Prep

·  Only install bolts after gasket and flange fit-up are verified.

·  Confirm gasket type/size and flange faces are cleaned before bolting starts threads should not be damage.

- Bolt Tightening Sequence & Torque Control

·  Bolts must be tightened in star or circular pattern to distribute load evenly.
·  Typically done in multiple passes: 1st pass at ~30% of torque, 2nd pass ~60%, Final pass ~100%

- Exposed Thread Requirement

·  After tightening, at least 2 full threads of each bolt must be visible outside the nut.

- Bolt Torque/Tension Documentation

·  All torque values, passes, and tools used must be recorded in the QC inspection report or Bolt data sheet.

- Valve Fit up:

- Correct Valve Type & Specification

·  Verify valve type, rating, size, material, and end connection matches the approved IFC isometric

- Visual & Physical Inspection:

·  Inspect overall physical condition for dents, cracks, damage, or corrosion.

- Valve Orientation / Flow Direction Check:

·  Many valves (check, globe, control, swing check) have a flow direction arrow on the body, ensure valve is installed with correct orientation relative to flow indicated on piping drawings.

- End connection:

·  It can be But weld, Socket Weld or flange is used
·  If flange we will check for gasket, bolting etc and if welded we will check for the alignments and angle

- Check for Test:
·  Hydro static seat test must be done before the installation of valves

- Fit-up Inspection of Spool:

·  Pipe alignment & fit-up check.

·  Fitting orientation & position.

·  Flange faces & alignment.

·  Gasket type & installation.

·  Valve orientation & connection fit.

·  Bolts/nuts torque & fit.

·  Line overall routing vs isometric.

·  Support, vents, drains, and exposed joints for testing.

- - Documentation:

- ·  Isometric Drawings / Spool Drawings

- ·  Inspection & Test Plan (ITP)

- ·  Material Test Certificates (MTCs)

- ·  Welding Procedure Specifications (WPS)

- ·  Welder Qualification Records (WPQ/WQT)

- ·  Fit-Up Inspection Checklists ie SAIC-L-2005/2006/2007 etc

- ·  NDT Reports

- ·  Bolt Torque/Tensioning Report

- ·  Calibration Certificates (for gauges & tools)